ICS 87.040

G 50

中华人民共和国国家标准

GB/T ×××××—××××/ ISO 13076:2012

色漆和清漆 涂层的目视评定方法和光照条件

Paints and varnishes —Lighting and procedure for visual assessments of coatings

(ISO 13076:2012,IDT)

(征求意见稿)

（本稿完成日期：2018-4-20）

×××× - ×× - ××发布

×××× - ×× - ××实施

前  言

本标准按照GB/T 1.1—2009给出的规则起草。

本标准使用翻译法等同采用国际标准ISO 13076:2012《色漆和清漆 涂层的目视评定方法和光照条件》。

本标准由中国石油和化学工业联合会提出。

本标准由全国涂料和颜料标准化技术委员会(SAC/TC5)归口。

本标准起草单位：

本标准主要起草人：

色漆和清漆 涂层的目视评定方法和光照条件

范围

本标准规定了对涂层表面或涂层内部的老化区域、斑点或其它缺陷进行目视评定的方法和光照条件。

本标准不适用于目视比色，目视比色可按ISO 3668的规定进行。

原则

在规定的光照条件下，对样板的老化区域、斑点或其它缺陷进行目视评定。

仪器设备

日光灯

装有能向下反射光线的镀铝反射膜的广角光源（见图1），色温为6500K，显色度为9（对应于显色等级1A，即显色指数Ra为90～100）。

该色温和显色度对应的灯色为965。

目视评定方法

总则

自然日光或人造日光都可用于常规评定。由于自然日光并不稳定，在自然日光下评定时会受周围环境的影响，因此仲裁评定应使用精确控制的人造日光。

自然日光下的评定

评定样板时，最好采用局部多云天气条件下的散射日光，并且样板朝北放置(在南半球时样板朝南放置）。用不低于2000 lx的光照度对待评定区域及其周围区域进行均匀照射。避免阳光直射。

人造日光下的评定

在3.1规定的人造日光下评定涂膜。测试时，离光源一定的距离托起样板，使样板表面的光照度不小于750 lx (见图 1)。

日光灯安装后应测量光照度。

样板评定时可向任何方向倾斜。在灯光产生的明暗交界处检查样板，最易识别样板老化区和斑点。

仲裁评定应在人造日光下进行。

测试报告

当使用本标准规定的方法时，试验报告应增加如下信息：

注明本标准编号（GB/T ×××××）；

指出评定试板时采用的光源类型（自然日光或人造光源）；若使用人造光源，应给出光源类型的详细信息。

说明：

1——灯。

灯、试板和观察人员的位置

（资料性附录）
应用示例

表 A.1列出了能使用本标准规定的方法进行目视评定的示例。

本标准应用示例

| 试验方法 | 标准 |
| --- | --- |
| 划格试验 | ISO 2409 |
| 耐冲击试验 | ISO 6272-1、 ISO 6272-2 |
| 抗石击性 | ISO 20567-1、 ISO 20567-2 |
| 耐化学介质性 | ISO 2812-1、 ISO 2812-2、 ISO 2812-3、 ISO 2812-4、 ISO 2812-5、 ISO 15710 |
| 涂膜缺陷 | ISO 4628-2、 ISO 4628-3、 ISO 4628-4、 ISO 4628-5、 ISO 4628-6、 ISO 4628-7、 ISO 4628-8、 ISO 4628-10 |
| 耐擦伤性 | ISO 1518-1、 ISO 1518-2、 ISO 12137 |
| 汽车清洗试验 | ISO 20566 |
| 弯曲试验 | ISO 1519、 ISO 6860、 ISO 17132 |
| 干燥试验 | ISO 9117-1、 ISO 9117-2、 ISO 9117-3、 ISO 9117-4、 ISO 9117-5、 ISO 9117-6 |
| 研磨细度 | ISO 1524 |
| 拉开法附着力试验 | ISO 4624 |
| 抗流挂性 | ISO 16862 |
| 与涂装过程有关的涂层体系性能评价 | ISO 28199-3 |
| 耐湿擦洗性 | ISO 11998 |

参 考 文 献

[1] ISO 1518‑1, Paints and varnishes — Determination of scratch resistance — Part 1: Constant-loading method

[2] ISO 1518‑2, Paints and varnishes — Determination of scratch resistance — Part 2: Variable-loading method

[3] ISO 1519, Paints and varnishes — Bend test (cylindrical mandrel)

[4] ISO 1524, Paints, varnishes and printing inks — Determination of fineness of grind

[5] ISO 2409, Paints and varnishes — Cross-cut test

[6] ISO 2812‑1, Paints and varnishes — Determination of resistance to liquids — Part 1: Immersion in liquids other than water

[7] ISO 2812‑2, Paints and varnishes — Determination of resistance to liquids — Part 2: Water immersion method

[8] ISO 2812‑3, Paints and varnishes — Determination of resistance to liquids — Part 3: Method using an absorbent medium

[9] ISO 2812‑4, Paints and varnishes — Determination of resistance to liquids — Part 4: Spotting methods

[10] ISO 2812‑5, Paints and varnishes — Determination of resistance to liquids — Part 5: Temperaturegradient oven method

[11] ISO 3668, Paints and varnishes — Visual comparison of the colour of paints

[12] ISO 4624, Paints and varnishes — Pull-off test for adhesion

[13] ISO 4628‑2, Paints and varnishes — Evaluation of degradation of coatings — Designation of quantity and size of defects, and of intensity of uniform changes in appearance — Part 2: Assessment of degree of blistering

[14] ISO 4628‑3, Paints and varnishes — Evaluation of degradation of coatings — Designation of quantity and size of defects, and of intensity of uniform changes in appearance — Part 3: Assessment of degree of rusting

[15] ISO 4628‑4, Paints and varnishes — Evaluation of degradation of coatings — Designation of quantity and size of defects, and of intensity of uniform changes in appearance — Part 4: Assessment of degree of cracking

[16] ISO 4628‑5, Paints and varnishes — Evaluation of degradation of coatings — Designation of quantity and size of defects, and of intensity of uniform changes in appearance — Part 5: Assessment of degree of flaking

[17] ISO 4628‑6, Paints and varnishes — Evaluation of degradation of coatings — Designation of quantity and size of defects, and of intensity of uniform changes in appearance — Part 6: Assessment of degree of chalking by tape method

[18] ISO 4628‑7, Paints and varnishes — Evaluation of degradation of coatings — Designation of quantity and size of defects, and of intensity of uniform changes in appearance — Part 7: Assessment of degree of chalking by velvet method

[19] ISO 4628‑8, Paints and varnishes — Evaluation of degradation of coatings — Designation of quantity and size of defects, and of intensity of uniform changes in appearance — Part 8: Assessment of degree of delamination and corrosion around a scribe or other artificial defect

[20] ISO 4628‑10, Paints and varnishes — Evaluation of degradation of coatings — Designation of quantity and size of defects, and of intensity of uniform changes in appearance — Part 10: Assessment of degree of filiform corrosion

[21] ISO 6272‑1, Paints and varnishes — Rapid-deformation (impact resistance) tests — Part 1: Falling weight test, large-area indenter

[22] ISO 6272‑2, Paints and varnishes — Rapid-deformation (impact resistance) tests — Part 2: Falling weight test, small-area indenter

[23] ISO 6860, Paints and varnishes — Bend test (conical mandrel)

[24] ISO 9117‑1, Paints and varnishes — Drying tests — Part 1: Determination of through-dry state and through-dry time

[25] ISO 9117‑2, Paints and varnishes — Drying tests — Part 2: Pressure test for stackability

[26] ISO 9117‑3, Paints and varnishes — Drying tests — Part 3: Surface-drying test using ballotini

[27] ISO 9117‑4, Paints and varnishes — Drying tests — Part 4: Test using a mechanical recorder

[28] ISO 9117‑5, Paints and varnishes — Drying tests — Part 5: Modified Bandow-Wolff test

[29] ISO 9117‑6, Paints and varnishes — Drying tests — Part 6: Print-free test

[30] ISO 11998, Paints and varnishes — Determination of wet-scrub resistance and cleanability of coatings

[31] ISO 12137, Paints and varnishes — Determination of mar resistance

[32] ISO 15710, Paints and varnishes — Corrosion testing by alternate immersion in and removal from a buffered sodium chloride solution

[33] ISO 16862, Paints and varnishes — Evaluation of sag resistance

[34] ISO 17132, Paints and varnishes — T‑bend test

[35] ISO 20566, Paints and varnishes — Determination of the scratch resistance of a coating system using a laboratory-scale car-wash

[36] ISO 20567‑1, Paints and varnishes — Determination of stone-chip resistance of coatings — Part 1: Multi-impact testing

[37] ISO 20567‑2, Paints and varnishes — Determination of stone-chip resistance of coatings — Part 2: Single-impact test with a guided impact body

[38] ISO 28199‑3, Paints and varnishes — Evaluation of properties of coating systems related to the application process — Part 3: Visual assessment of sagging, formation of bubbles, pinholing and hiding power

_________________________________